## Slide 1: Technical Project Exhibition on
Introduction
Microstructural And Corrosion Behaviour Of Al-2024/Sic/Cenosphere Hybrid Metal Matrix Composites
Composite materials are playing vital and major role in research and development of various engineering and aeronautical sectors because of obtaining superior properties such as higher specific strength, high hardness, high wear resistance, high thermal resistance and low density. Specifically aluminum metal matrix composites have preferred in aeronautics, marine and automotive industries for obtaining best result of mechanical properties.
Scope of the Project
In the project Al 2024 reinforced with varying weight percentages of Sic and constant weight percentage of Cenosphere were considered to improve:-
the mechanical properties of Al2024 based metal matrix alloy. And
Corrosion Behaviour
Methodology
The Flow Chart explains the procedure followed in the project:-.
Literature Review
Selection of Matrix & Reinforcement Materials
Manufacturing of Metal matrix composites by Stir Casting Method
Determination of Mechanical Properties of Prepared Composites
Specimen Characterization
Tensile Test
Hardness Test
Wear Test
Optical Microscope
SEM
Corrosion Studies
Salt Immersion Test
Salt Spray Test
Bablu Kumar Yadav, Guddu Kumar Yadav , Roshan Kumar Ranjan , Deepak B R, Mr. Balaji Y S
Department of Mechanical Engineering
Nagarjuna College of Engineering and Technology
Results
Evaluation of Microstructure:-
Compression Test:-
Load v/s Displacement of Al-2024
Load v/s Displacement of Al-2024 +2% SiC+5% Cenosphere
Load v/s Displacement of Al-2024 +4% SiC+5% Cenosphere
Load v/s Displacement of Al-2024 +6% SiC+5% Cenosphere
Load v/s Displacement of Al-2024 +8% SiC+5% Cenosphere
Chart: 
| 0 | 2 | 4 | 6 | 8
Compression strength | 0.167 | 0.587 | 0.59 | 0.632 | 0.654
Column1
Column2
% Reinforcement
Compression strength
Figure : Compression Strength v/s % of reinforcement
Specimen | Ultimate Load (KN) | Displacement (mm) | Compression Strength (KN/mm2)
Al 2024 | 81.9 | 6 | 0.167
Al 2024+ 2% SiC+ 5% Cenosphere | 77.88 | 7.4 | 0.587
Al 2024+ 4% SiC+ 5% Cenosphere | 78.3 | 6 | 0.59
Al 2024+ 6% SiC+ 5% Cenosphere | 83.86 | 5.2 | 0.632
Al 2024+ 8% SiC+ 5% Cenosphere | 86.82 | 6 | 0.654
Hardness Test
Material | Trail No. | Force Applied in Kgs | Time in Sec | Diameter of Indentation d (mm) | Average diameter of Indentation | BHN(Kgf/mm²)
Al 2024 +0% SiC +5%Cenosphere | 1 2 3 | 187.5 | 10 | 2.1 2.0 2.0 | 2.03 | 45.87
Al 2024 + 2% SiC+ 5%Cenosphere | 1 2 3 | 187.5 | 10 | 2.0 2.1 2.1 | 2.06 | 44.06
Al 2024 + 4% SiC+ 5%Cenosphere | 1 2 3 | 187.5 | 10 | 2.0 2.0 2.0 | 2.0 | 47.74
Al 2024 + 6% SiC+ 5%Cenosphere | 1 2 3 | 187.5 | 10 | 1.8 1.6 2.0 | 1.8 | 62.40
Al 2024 + 8% SiC+ 5%Cenosphere | 1 2 3 | 187.5 | 10 | 1.5 2.0 2.0 | 1.83 | 59.92
Salt Spray Test
SL NO | Material | Initial weight(grams) | Final weight(grams)
1 | AL-2024 (Pure) | 33 | 32
2 | AL-2024,5% Cenosphere & 2% Sic | 34 | 34
3 | AL-2024,5% Cenosphere & 4% Sic | 33 | 32
4 | AL-2024,5% Cenosphere & 6% Sic | 34 | 33
5 | AL-2024,5% Cenosphere & 8% Sic | 30 | 31
Salt Immersion Test
Scope For Future Work
Further Investigation can be carried out
By different manufacturing processes like powder metallurgy route and Spray casting to analyze for better properties.
By increasing the percentage of Cenosphere which was kept as 5%constant in present investigation.
By enhancing the tribological properties of the composite composition mixture by heat treatment processes.
Conclusion
Images from optical microscope of composites of various compositions were obtained, where we can clearly observe uniform distribution of particles, grain boundaries and little porosities showing good quality casting.
The Compression strength and Hardness increased with increase in weight fraction of Silicon carbide.
Prepared composites subjected to different test like salt immersion test, salt spray test and potentiodynamic polarization test showed significant improvement in corrosion resistance.
0%SiC
2% SiC
4% SiC
6% SiC
8% SiC